  - DECLARATION OF PERFORMANCE

DoP No. 019 BK-MicroGrund Universal

Universal structural base with microfibers

- Name and/or designation of the construction product type:

BK-MicroGrund Universal

- Type, batch or serial number or some other element that enables identification of the construction product:

Stamped on the packaging.

- Intended use or uses of the construction product in accordance with the appropriate technical specification or technical regulation:

Universal structural substrate with microfibers intended for leveling, neutralizing, strengthening and waterproofing of the substrate before applying all types of facade paints and decorative plasters, except for silicate paints/plasters. It is suitable for filling fine cracks and additional reinforcement of the substrate.

- Manufacturer's name and address:

Banja Komerc Bekament DOO,

132 Kralja Petra Prvog Str.,

34304 Banja, Aranđelovac, Serbia

- Name and address of representative: /

- System or systems of assessment and verification of the constancy of performance of the construction product (AVCP), determined by the appropriate technical specification or technical regulation:

System 4

- Applied technical regulations:

/

- List of essential characteristics and performance of essential characteristics:

| Characteristics | Value | Specification |
| --- | --- | --- |
| Density, kg/dm3 | 1,55-1,75 | EN ISO 2811-1 |
| Adhesion to the substrate, MPa | ≥ 1,0 | EN ISO 4624 |
| Water absorption, kg/m2 h0,5 | < 0,2 (W2 according to EN1062-1) | EN 1062-3 |
| Maximum particle size, µm | < 1500 | ISO 787-7/EN ISO 787-18 |
| VOC-content, g/l | < 1 | max.allowed value A(g), 30 g/l |

- Product testing was conducted by the Institute for Material Testing a.d. in Belgrade and the Test Report under number 1155/06, September 2006, was issued.

The characteristics of the product are in accordance with the characteristics specified in point 8.

This performance declaration is published in accordance with the Law on Construction Products (Official Gazette of RS, No. 83 of 29 October 2018) and EU Regulation, CPR 305/2011 and is solely the responsibility of the manufacturer specified in point 4.

Vesna Jovanović, BSc in Technology Eng.

Director of development and technical support

In Banja

07.07.2023.

Signed

Round official seal: BANJA komerc BEKAMENT DOO V

Banja Aranđelovac